Hi Speed snow white is an uncoated ultra-smooth board ideal for quality offset printing.

Suitable for brochure, name card, menu, commercial tag, greeting card and file folders.

Economical and easy to use.

| SPECIFICATIONS |  |  |  |  |
| --- | --- | --- | --- | --- |
| Characteristics | Units | 250g/m2 | 300g/m2 | Test Method |
| Basis Weight | g/m2 | 250 ± 4% | 300 ± 4% | T410 om-98 |
| Thickness | ㎛ | 278 ± 6 | 340 ± 7 | T411 om-97 |
| Smoothness | sec/10ml | 45 ± 10 | 40 ± 10 | T479 om-91 |
| Opacity | % | ≥ 99 | ≥ 99 | ISO 2471-1999 |
| Wax Pick | °A | ≥ 16 | ≥ 16 | T59 om-93 |
| Moisture | % | 5.8 ± 0.5 | 5.8 ± 0.5 | T412 om-94 |

Note:	 The specifications refer to an average of a composite sample according to our standard procedures.

Not to be used for purposes other than what we specified. We reserve the right to modifications.

Exclusively distributed by:

KPP-Antalis (Malaysia) Sdn Bhd

Level 3A, Wisma Comcorp,

37, Jalan Pelukis U1/46, Section U1

Temasya Industrial Park, 40150 Glenmarie Shah Alam

Selangor Darul Ehsan

T +603 7627 8300   F +603 7627 6163

E info.my@kppantalis.com